# CNC Cutting Recipe Formula Table

Metric formulas used to turn machine, cutter, material, and operation data into a safe starting recipe

The equations are shared across materials. What changes between wood, metal, and plastics is the recipe data supplied to them: cutting speed, chip load, specific cutting force, thermal limits, and safe engagement. The calculator chooses the lowest safe limit; it does not treat a material as one universal hardness number.

# Core formulas

| Formula | Metric equation | Purpose in the recipe |
| --- | --- | --- |
| Cutting speed | Vc = (π x D x N) / 1000 | Edge speed in m/min. The material recipe provides a target Vc range. |
| Spindle speed | N = (1000 x Vc) / (π x D) | RPM calculated from target cutting speed and cutter diameter. |
| Feed rate | F = fz x Z x N | XY feed in mm/min. Uses chip load per tooth, flute count, and RPM. |
| Chip load | fz = F / (Z x N) | Thickness of material removed by one tooth, in mm/tooth. |
| Material removal rate | MRR = ae x ap x F | Volume removed in mm3/min. ae is stepover; ap is pass depth. |
| Approx. cutting power | P = (Kc x MRR) / (60,000 x η) | Power in W. Kc is specific cutting force; η is drivetrain efficiency. |
| Safe pass depth | ap = min(recipe, tool, machine, stock) | Lowest safe DOC limit from the recipe, cutter geometry, machine envelope, and remaining stock. |
| Machining time | T = L / F | Approximate cutting time in minutes for path length L in mm. Rapids and entry moves add time. |

## Symbols

| Symbol | Meaning |
| --- | --- |
| Vc | cutting speed, m/min |
| D | cutter diameter, mm |
| N | spindle speed, RPM |
| F | XY feed rate, mm/min |
| fz | chip load, mm/tooth |
| Z | number of flutes |
| ae | radial engagement or stepover, mm |
| ap | axial depth of cut or DOC, mm |
| Kc | specific cutting force, N/mm2 |
| η | usable drivetrain efficiency, 0 to 1 |
| L | cut path length, mm |

# Material specific recipe math

Each material family supplies different engineering inputs to the same core equations. Hardness is useful, but it is not a shared number across wood, metal, and plastics.

| Material | Recipe inputs | RPM and feed inputs | DOC limiter | Main concern |
| --- | --- | --- | --- | --- |
| Softwood | Janka hardness, density, moisture, grain direction | Vc = Vc_wood; fz = fz_wood | ap = min(tool, grain finish, machine, stock) | Avoid tear-out and over-aggressive full-width slotting. |
| Hardwood | Janka hardness, density, moisture, grain direction | Vc = Vc_hardwood; fz = fz_hardwood | ap = min(tool, force/deflection, finish, stock) | Higher cutting force than softwood; reduce engagement first. |
| Plywood / MDF | Sheet density, glue/void risk, dust evacuation | Vc = Vc_sheet; fz = fz_sheet | ap = min(tool, glue abrasion, machine, stock) | Use conservative recipe data because glue, veneers, and voids vary. |
| Aluminium | Alloy, temper, Brinell/Rockwell hardness, cooling | Vc = Vc_alloy; fz = fz_metal | ap = min(tool, Kc/power, deflection, chip evacuation) | Kc and spindle power are important; chip evacuation is mandatory. |
| Brass | Alloy, Brinell/Rockwell hardness, cutter geometry | Vc = Vc_brass; fz = fz_brass | ap = min(tool, Kc/power, chatter, stock) | Often more forgiving than aluminium, but verify the alloy recipe. |
| Acrylic | Softening temperature, cutter type, chip evacuation | Vc = Vc_acrylic; fz must avoid rubbing | ap = min(tool, thermal limit, chip evacuation, stock) | Thermal behaviour is the main risk: chips must carry heat away. |
| HDPE | Softening temperature, flexibility, cutter type | Vc = Vc_hdpe; fz must avoid rubbing | ap = min(tool, heat, material flex, stock) | Control heat and deflection; use a recipe that creates chips rather than dust. |
| Foam | Density, cell structure, desired finish | Vc = Vc_foam; fz = fz_foam | ap = min(tool, finish, part stability, stock) | Surface quality and part stability usually limit the recipe before power. |

## Why material recipes differ

Wood uses Janka hardness with density, moisture, and grain. Janka alone does not predict tear-out or dust evacuation.

Metals use alloy and temper plus Brinell or Rockwell hardness. Their recipe needs specific cutting force Kc so the spindle-power and force limits can be checked.

Plastics use thermal behaviour as a primary input. The recipe must prevent rubbing and melting, not merely limit cutting force.

All recipes are calibrated to a machine and spindle envelope. An AltMill and LongMill receive separate validated limits, not a simple multiplier.

# Recipe calculation sequence

| Step | Action | Calculation / rule |
| --- | --- | --- |
| 1 | Identify | Resolve machine/spindle, cutter geometry, material family, and operation. |
| 2 | Select material data | Load source-controlled target Vc, fz, Kc, thermal/finish factors, DOC, and WOC limits. |
| 3 | Calculate RPM | Use cutter diameter and Vc. Snap to a real router speed, then clamp to installed spindle limits. |
| 4 | Calculate feed | F = fz x Z x N. If RPM is clamped, recalculate F so chip load stays intentional. |
| 5 | Choose engagement | Select operation-specific stepover ae and pass depth ap; slotting is more restrictive than low-engagement pocketing. |
| 6 | Apply limits | Reject or reduce values exceeding usable flute length, machine feed, cutting power, deflection, thermal, or stock limits. |
| 7 | Choose entry | Prefer ramp/helical entry where possible. Limit vertical plunge by material recipe and machine Z capability. |
| 8 | Store result | Save resolved values with recipe/profile revision, constraints applied, and confidence. Never rewrite old jobs silently. |

## Pass depth decision

DOC is not calculated from hardness alone. The implementation takes the lowest applicable value:

| Limit source | What it protects |
| --- | --- |
| Material recipe | Maximum axial engagement proven for the material, cutter family, and operation. |
| Tool geometry | Cutter diameter, usable cutting length, flute count, and stick-out. |
| Operation | Slot/profile/pocket/surfacing/V-carve all produce different radial engagement and force. |
| Machine and spindle | Tested feed, force/deflection, and usable spindle-power envelope. |
| Stock | Remaining depth, workholding, and the need to preserve a finish pass. |

## Practical rule for gCAM

The normal user chooses machine, tool, material, and operation. gCAM calculates a conservative starting recipe. Advanced users may override the numbers, but the automatic path remains source-backed, machine-aware, and traceable.